## Slide 1: Work on Afera Test Methods
Overview
Status May 18 2022

## Slide 2
 |  |  |  | Questions, general | 
 |  |  |  | Better word for referee testing: arbitration tests Standard conditions 23+/- 1? Most ENs say +/- 2 Greatest difference; right word? Explanations of abbreviations in each method. Necessary? | 

## Slide 3
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
5001 | GTF 6004, PSTC 101 12/13 | Peel | A | Mostly identical to PSTC 101 12/13. Made few changes, adoptions from PSTC 101. no change to peculiarities that are in 101, also. Referenced standards differ in names from the PSTC version 2022-04-11 Figures must be checked separately No conditioning times in PSTC and ISO either, rationale behind? Changes Changed title Added statement to „1. Scope“, from PSTC 101 Added speed to 1.1.1, from PSTC 101 Added full titles to Ref. Doc. In 2. Changed Note 1 in 5.1, closer to PSTC 101 Changed „mass“ to „pressure“ in 5.4.7 – same in PSTC 101 Added 7.2 no of tests, adopted from PSTC 101 | Ready for upload 2022-05-05 Sent for upload 2022-05-18
 |  |  |  | Comments on pictures/drawings Drawings necessary to understand the text, order of figures may need to be changed another time | 

## Slide 4
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
5004 | GTF 6005 = PSTC 131 = | Breaking Strength and Elongation of Adhesive Tapes | A | Contents and language almost 100 % in line with PSTC 131, except title. Figure 1 added, Zwick, right picture? Speed in 5004 wrong, corrected. Not changed: odd terms, e.g. „relative strength“ in 4.2 The whole text must be checked against real life! 2022-03-20 Conditioning time taken out again, not in Appendix A of PSTC manual. Changes: corrected names of reference documents (clause 2) Added „or“ in Note 3 to make text understandable Removed phrase „it is common“ in 6.2 Corrected rate of extension in 10.1.2 (critical mistake) added 11.2.2., text is from PSTC131. 2022-04-19. Removed „significant places“ in 12.1.4 and 12.2 Few formalities | Ready for upload 2022-04-28 Sent for upload 2022-04-29
 |  |  |  | Comments on pictures/drawings Not sure whether Fig 2 is showing what is meant by the text (mention Source: Zwick ok?), to be clarified in WG | 

## Slide 5
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
5012 | GTF 6006, PSTC 107 | Static Shear | A | Text is mostly identical to PSTC 107. This includes the critical mistake that is in both versions: the assigment of the test masses to the procedure variants in 5.5.4. corrected Statements that seem peculiar, difficult to understand, e. g. 12.1.8 - not corrected Changes Added/corrected full titles to Reference documents in 2. Changed some wording in clause 3. Adopted phrase from PSTC107 in 4.3.2 Corrected panel size in 5.3.1, adaptation of values in PSTC 107 Corrected assignemt of variants to test masses in 5.5.4.1 critical mistake – to be rechecked as this is mistake in PSTC 107, too Changed few words in 9. Added panel drying time in 10.2.1, adopted from PSTC 107 10.2.3 procedure of roll down needs to be clarified, different from PSTC 107 Remove „five“ as no of specimen in 11.1 as this is in contrast to 7.1 Few words in 12.1.3 | Ready for upload 2022-05-06 Sent for upload 2022-05-18
 |  |  |  | Comments on pictures and drawings Needs separate revision | 

## Slide 6
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
5013 | GTF 6001 PSTC 17 12/13 | SAFT | A | Text is mostly identical to PSTC 17, very few changes made, adoptions from PSTC17. Changes Added/corrected full titles of Reference documents in clause 2. Adopted statement on quality of panels from PSTC 17 in 5.3.1 Few formalities in clauses 6 -12 Note: 12.6 is different in content from PSTC 17, not changed | Ready for upload 2022-05-06 Sent for upload 2022-05-18
 |  |  |  | Figures must be checked separately 2022-4-11 | 
5006 | GTF 6002 = PSTC 133 = EN1942:2003 | Thickness of Adhesive Tapes | A | Contents almost 100 % in line with PSTC 133, language also. Results Clause is missing in both versions. Changes: Few differences in language, adopted phrases from PSTC 133 Formalities in 2., corrected titles of ASTM standards No changes in contents | Ready for upload 2022-04-25 Sent for upload 2022-04-25
 |  |  |  | Comments on pictures/drawings Picture in 5006 must be changed, gauge foot must be smaller than width of tape. 2022-03-14. Picture exchanged by new one from tesa 2022-03-16 = The major change to the method | 

## Slide 7
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
 | GTF 6003 | Guidelines on Width and Length | A | Text is identical to PSTC 71, Changes: corrected 5.3.1 and 5.3.2 which are wrong in PSTC 71 as well. 2022-04-11 Corrected names in „9. Reference Documents“ Remark: Why no reference to Afera in „10. Comments“? Should be added. | Ready for upload 2022-04-28 Sent for upload 2022-04-29
 |  |  |  | Comments on pictures/drawings Not relevant | 

## Slide 8
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
5014 | GTF 6007, PSTC 16 | Loop Tack | A | Text appr. 80% identical to PSTC 16. differences: PSTC has 2 methods described, Afera is more specific on determination of results, only very few changes made so far. 2022-04-11 Figures must be checked separately. Missing: Clause 2 Reference documents, not in PSTC 16 either Should we add it or better let the method as close to current GTF as possible? Changes Added no of Peel test method in 4.3 Added conditioning time in 7.1 (same as in PSTC) Few formalities (e. g. N instead of Newtons) | Ready for upload 2022-05-04 Sent for upload 2022-05-18
 |  |  |  | Comments on drawings/pictures Pictures necessary to understand the text, pictures seem to be very instructive, to be rechecked separately | 

## Slide 9
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4003 | EN 12024 | Resistance to High Temperature and Humidity | B | The contents are 100% in line with EN 12024, the description seems odd, description of desiccator as means of climate definition, climate chamber added as option. Why had the author removed that? It is in EN 12024!! 2022-02-24 Changes Added 3.4 climate chamber“ Moved 6.4 to 7.1, for clarity Removed some redundant phrases in clause 7 Reformulated „8. Test Report“ Some formalities | Ready for upload 2022-05-01 Sent for upload 2022-05-03
 |  |  |  | Comments on pictures/drawings No picture/drawing necessary, from my point of view We could have a picture of a desiccator with rolls from PSTC manual | 

## Slide 10
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4007 | EN 12025:1996 | Tearing Strength of Adhesive Tapes by the Pendulum Method | C | Text in major parts identical to EN12025, major difference in content: 4007 restricted to cloth tape, 12025 not (however, focus on cloth). order of the sections differ sometimes, most of the contents appear identically in both standards Changes Added full titles of Reference Documents in clause 2. Added the no of specimens to be tested (7.2.1) Added phrase on reporting separately warp and weft directions in 10.3 Few formalities | Ready for upload 2022-05-02 Sent for upload 2022-05-03 Not fully understood the method, check at tesa?
 |  |  |  | Drawings show the apparatus described in the text, cannot be replaced by photo of more modern machine Perhaps, photo can be added from PSTC manual | 
4007Spple | EN12025:1996 Annex A |  | C | Same as 4007, changed 7.2. and 7.3 for clarity, closer to description in EN12025 Added 7.1 Changed some wording in 7.2., 7.3 and 7.4 for better clarity Added phrase on reporting separately warp and weft directions in 8.2 Few formalities | Ready for upload 2022-05-02 Sent for upload 2022-05-03
 |  |  |  | Comments on pictures/drawings Drawing necessary to understand the text. | 

## Slide 11
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4008 | EN12026:1996 | Measurement of the Unwinding Force of Adhesive Tapes at High Speed | A | Contents are 100% in line with EN12026, Text seems odd. Picture introduced (ex tesa) Changes Title – see left Clarified “1 scope“, Clarified „3 apparatus“, Added „7 Report“ – as it is in EN12026 | Ready for upload 2022-04-30 Sent for upload 2022-05-03
 |  |  |  | Comments on pictures/drawings The text has no reference to pictures/drawings Picture for illustration, provided by tesa | 

## Slide 12
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4009 | EN 12027 | Flame Resistance of Adhesive Tapes | A | Contents almost 100 % in line with EN 12027, except drawings. 2022-03-16 Changes: Added names of standards in 2. Changed „4 significance and use“ Added 5.4 Replaced „hood“ by „test chamber“ in 5. Changed 9.1.3 so that it is in line with 12027. | Ready for upload 2022-04-28 Sent for upload 2022-04-29
 |  |  |  | Comments on pictures/drawings Drawings not 100 % necessary, from my point of view. The method is also described in DIN EN 60454-2. Drawing there is wrong, 16 holes, instead of 12 in the text. There is a drawing in 12027, poor quality. No picture available from tesa | 

## Slide 13
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4010 |  | Determination of Insulation Resistance | A | Not found any equivalent method yet. Text difficult to understand. Changed only formalities so far. Method in use at tesa? Not in use! 2022-03-19. A similar method to this one is described in ASTM D1000, clause 91-96 Changes Added full title of reference document in 2. Changed some wording in the text | Ready for upload 2022-05-03 Connection of figures and text to be rechecked separately
 |  |  |  | Drawings mandatory to understand the method. What are sections A A and B B (Figure 2)? | Sent for upload 2022-05-03

## Slide 14
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4011 | DIN EN 60454-2, clause 17 | Electric Strength of Adhesive Tapes | A | Same drawing as in 4011 is in IEC 60243-1, p 20! In my opinion, the text is hard to understand. Results and report mixed, separated in the amended version. The same mix is found in 60243-1, however! 2022-03-16. Suggestion to remove 6.4 as it does contribute to confusion. Changes: Few changes in words/phrases Added clause „9. Results“ Few formalities | Ready for upload 2022-05-03 Sent for upload 2022-05-03
 |  |  |  | Comments on drawings/pictures The drawing is necessary as there is no written description of the apparatus, just 4.2.1.: „A suitable device is shown in Fig. 1“ The drawing is almost identical to the one in 60243-1 (p. 20). There is a photo available from Coro, showing the device. | The method needs to be discussed with expert on electriacl methods

## Slide 15
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4013 | EN 1944:1996 | Unwind Adhesion of Adhesive Tapes at Low Speed | A | Title to be changed? Title is identical to EN1944. Content and language are almost identical to EN 1944 English version. 23 +- 1 °C is this correct? To be checked. Changes Adapted „1. scope“ to EN 1944:1996 Changed speed in 3.1.2, critical mistake Clarified 5.4, adapted to EN 1944 Added „7. Report“ Changed picture, see below | Ready for upload 2022-05-01 Sent for upload 2022-05-03
 |  |  |  | Comments on pictures/drawings Can the drawing be replaced by the photo? 22-03-10 Replaced the drawing by the photo, 2022-05-01 | 
4014 | EN 12028:1996 | Elongation of Adhesive Tapes under Reduced Load | C | Method seems outdated to me. EN 12028 has a section „Report“, 4014 does not have it. => added all other parts are almost 100% in line witth EN12028, exept for the title: 12028 is „… under static load“ 2022-03.11 Changes: Some wording in „1. scope“ Added „3.5 stop-watch or other timer“ Added „7. Test Report“ – same as in EN12028 | Ready for upload 2022-05-01 Sent for upload 2022-05-03
 |  |  |  | Comments on pictures/drawings No picture necessary | 

## Slide 16
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4015 | EN 1945 | Quick Stick | C | Content in line with EN1945, cleaning proecedure shortened through reference to Afera 5001. Open point both in 4015 and 1945: no reference marks mentioned in description of steel plates but mentioned in procedure. What to do? Is it really clever to work on the method and update it? Changes Added „2. Terms and definitions“ Changed wording in „3. Summary of Test Method“ Changed speed in 4.1.2, critical mistake Changed speed in 6.4, critical mistake Changed few words/phrases in clauses 6, 7, Added „8. Test Report“ | Ready for upload 2022-05-01 Sent for upload 2022-05-03
 |  |  |  | Comments on pictures/drawings No picture necessary, from my point of view EN1945 has a drawing Picture may be taken from PSTC-5 (fig 3), this is similar to the drawing in EN1945 | 

## Slide 17
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4019 | EN 12032 | Bond Separation of thermosetting Tapes during Curing | C | Seems outdated. Should we touch this method at all???? Text is mostly identical to EN 12032. Difference again in std climate: 23 +- 1 instead of 2!. Changes Reformulated „1. Scope“ transferred parts of it to New clause: „2. Terms and Definitions“ Added sentence to „3. summary of Test Method“ for clarification. Added 4.4 „weights“ Changed few words in 6. Added „8. Test Report“ Formalities, e.g. new numbering due to introduction of „Terms and Definitions“ | Ready for upload 2022-05-01 Sent for upload 2022-05-03
 |  |  |  | Comments on pictures/drawings 4019 has no drawings, while 12032 has 4 (!) to illustrate the sample preparation process. Could be helpful but would overly put focus on this method, in my opinion. | 

## Slide 18
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4021 | EN 12034:1996 | Length of a Roll of Adhesive Tape |  | Text almost identical to EN12034:1996. Changes: Introduced Conditioning clause 5.1 (taken from 12034) Corrected formula 2 in 6.1 Changed the order of the text in „scope“ Few formalities 2022-04-24 | Ready for upload 2022-04-24 Sent for upload 2022-04-25
 |  |  |  | Comments on pictures/drawings Drawing not necessary, from my point of view. It is the same one as in EN12034. Seems very old to me. The addtional info is zero. | 

## Slide 19
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4022 | EN 12035:1996 | Flagging or End Lifting Test | A | Drawing is mandatory for method but missing in Manual, to be renewed and added. Contents odd in some points (6 and 12 mm rod; cut to 9 mm width - why?) but 100% in line with EN12035. 2022-02-24. In line also with English version. including language, 2022-03-02. Method also in DIN EN 60454 difference only Fig 4! Changes Title Reformulated „1. Scope“, closer to EN12035 Transferred parts of scope to newly added „3. Terms and Definitions“ Added full titles of Reference Documents in 2. Changed numbering of clauses due to addition of clause 3. Changed few words in subsequent clauses | Ready for upload 2022-05-02 Sent for upload 2022-05-03
 |  |  |  | Comments on pictures/drawings The drawings, Fig. 1 – 4 are essential to understand the text. Missing in Manual (got lost from 2008 version) Fig 4 is wrong (flag too long), critical mistake, figures must be re-introduced and Fig 4 corrected. | 

## Slide 20
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4023 | EN 12036 | Solvent Penetration of Masking Tapes | C | Method significant? In use? Text not identical but very similar to EN12036. Roller described slightly different from EN12036. 2022-04-03 Changes Added „masking“ to scope Added 4.4 Added conditioning time in 7.1 (same as in 12036) Few formalities, added titles to Reference Documents 2022-04-25 | Ready for upload 2022-04-25 Sent for upload 2022-04-29
 |  |  |  | Comments on pictures/drawings No pictures/drawings necessary. | 
4026 |  | Accelerated Ageing of Adhesive Tapes | B | Rewritten the text. However, content and language are so weird that I think deletion of the method should be an option. Otherwise, the method would have to be built up from scratch. The current status is not a test method, more some general guidelines and statements how to approach and what to observe when accelerated ageing is to be done. | Ready for upload 2022-04-29 Sent for upload 2022-04-29
 |  |  |  | Comments on pictures/drawings No pictures/drawings necessary. | 

## Slide 21
Afera | DIN/EN/ISO/PSTC …. | Title | Category | Comments | 
4027 |  | Measurement of Width of Adhesive Tapes |  | Changed only few formalities. Language check and improvements with Bathsheba 2022-04-28. | Ready for upload 2022-04-29
 |  |  |  | Comments on pictures/drawings No pictures/drawings necessary. | Sent for upload 2022-05-03
4028 |  | Sampling Plan |  | Relevant? What is the meaning of: (unknown variability - single spec limit ) | 
4028Sppl |  |  |  |  | 

## Slide 22
Afera GTF | PSTC | latest version | EN | latest version | ISO | latest version
5001 6004 | 101 | 2013 | 1939 | Not found in Beuth | 29862 | 2018-05
5004 6005 | 131 | 2007 | 14410 | Not found in Beuth | 29864 | 2018-05
5012 6006 | 107 | 2007 |  |  | 29863 | 2018-05
5013 6001 | (17) | (2012) |  |  |  | 
5006 6002 | 133 | 2007 | 1942 | 2008 |  | 
5014 6007 | (16) | (2013) |  |  |  | 
GTF 6003 | (71) | (2013) |  |  |  | 
Standards equivalent to Afera standards, latest versions - GTFs

## Slide 23
Afera | PSTC | latest version | EN | latest version | ISO | latest version
4003 |  |  | 12024 | 1996 |  | 
4007 |  |  | 12025 | 1996 |  | 
4007 supplement |  |  | 12025 Annex | 1996 |  | 
4008 |  |  | 12026 | 1996 |  | 
4009 |  |  | 12027 | 1996 |  | 
4010 |  |  |  |  |  | 
4011 |  |  |  |  |  | 
Standards equivalent to Afera standards, latest versions – no GTFs

## Slide 24
Afera | PSTC | latest version | EN | latest version | ISO | latest version
4013 |  |  | 1944 | 1996 |  | 
4014 |  |  | 12028 | 1996 |  | 
4015 |  |  | 1945 | 1996 |  | 
4019 |  |  | 12032 | 1996 |  | 
4021 |  |  | 12034 | 1996 |  | 
4022 |  |  | 12035 | 1996 |  | 
4023 |  |  | 12036 | 1996 |  | 
Standards equivalent to Afera standards, latest versions – no GTFs

## Slide 25
Afera | PSTC |  | EN |  | ISO | 
4026 |  |  |  |  |  | 
4027 |  |  |  |  |  | 
4028 |  |  |  |  |  | 
4028 Supplement A |  |  |  |  |  | 
Standards equivalent to Afera standards, latest versions – no GTFs